Technical Specification Requirement

Type:   S-PVC

This Specification is suitable for homopolymeric PVC obtained by the suspension polymerization process for rigid extrusion of window or other profiles.

K-VALUE					66 – 68		ISO 1628-2

(DIN 53726)

BULK DENSITY		g/l		550 – 610		ISO 60

(ASTM D 1895-96)

RESIDUAL VCM		ppm		≤ 1			ASTM D 3749

(ISO 6401)

VOLATILE MATTER	%		≤ 0,3			ISO 1269

(ASTM D 3030-95)

PARTICLE SIZE

>    63 µm				%		≥ 95 – 98		ISO 4610

(ASTM D 1921A)

>  250 µm				%		≤  3 – 5		ISO 4610

(ASTM D 1921A)